- PennDOT SR 3032 GRS-IBS Bridge Project

- Construction Date

  - June 2017

- Concrete Masonry Units Required

Solid/Hollow	Color	Face Type	Corner	Unit	Quantity	Size

  - Solid 		Red	Split		No		910		8”x8”x16”

  - Solid		Red	Split		Yes		22		8”x8”x16”

  - Solid 		Gray	Split 		No		22		8”x8”x16”

  - Hollow 		Gray	Split 		No		855		8”x8”x16””

  - Hollow 		Gray	Split 		Yes		30		8”x8”x16”

  - Solid		Gray	Split 		Yes		6		8”x8”x16”

  - Solid 		Gray	Split 		No		94		8”x4”x16”

- Specifications

  - Freeze thaw testing in accordance with ASTM C1262-10 to establish conformance with ASTM C1372.

  - Compressive Strength = 3000 PSI Minimum.

  - Water absorption less than or equal to 5% after 24 hours.

  - Nominal dimensions = 8”x8”x16” Small CMU

  - Height tolerance: 1/16”, Length and width tolerance: 1/8”

  - Minimum face shell thickness: 1 ¼”

  - Minimum web thickness: ¾”

- Delivery Schedule

  - On or before June 1, 2017

- Delivery Location

##### Clearfield County:

  - 1905 Washington Ave 
PO Box 245 
Hyde, Pa. 16843

814-765-0524