2018 Inlet Repair Agreement
Specifications

Objective

The Pennsylvania Dept. of Transportation, Allegheny County is seeking to establish an agreement for the removal and replacement of the top portion of inlets of varying types throughout the County.

Statement of Work

All Quantities are estimated

Estimated quantity per type of inlet:

- Type M   		7 each

- Type C 			41 each

- Type S			1 each

- Type D-H Level 	2 each

Vendor Expectations

The awarded vendor will be expected to supply all materials, labor, and support for the removal and replacement of inlet tops. This includes traffic safety devices, heavy equipment, trained and qualified operators, operator safety devices, equipment mobilization and all other functions typically associated with an inlet repair job.

Standards

Inlets to be repaired will be up to 16” deep.

Inlets repaired under this agreement will be of type M, S, C, C-Alternate, D-H, or D-H Level

Typical Progression of Work

An estimated progression of work for this agreement will proceed as follows:

- Setup all traffic control and safety devices necessary to comply with Federal, State, and Local regulations.

- Remove the inlet grate and set it aside.

- Perform a thorough cleaning of the inlet removing all silt, gravel, debris, and any other materials or objects that could hinder the inspection of the inlet box to determine removal limits. The method of cleaning will be left to the vendor’s discretion.

- Remove unsound concrete until a sound base has been reached, as directed by the engineer.

- Cast-in-place or position the replacement precast inlet top in accordance with the RC Standards, and PA Publication 408, Section 607.

  - If casting in place, use an epoxy bonding compound compliant with PA Bulletin 15.

  - If using a pre-cast inlet top, use a non-shrink grout compliant with Section 1080.2

- Set the finished elevation of the new inlet top flush with the roadway.

  - If replacing a sunken/failed inlet, vendor should use an eight-foot straight edge or longer to establish a level top to the inlet.

Material

- Materials must comply with PA Publication 408/2016, Section 605.2

Measurement and Payment

Units of measurement will appear on the solicitation documentation and resulting Purchase Order as “Each”. The following measurements will be understood to be equivalent to “Each” or “EA.” for their respective materials:

Inlet Repair 		1 inlet repair job = 1 each

Depth Surcharge:	1 inch of depth surcharge = 1 each

Asphalt Surcharge:	1 cubic foot of asphalt = 1 each

All cleaning and removal of unsound concrete, epoxy coated reinforcing, new concrete, new pre-cast inlet top, grout, and all other work to remove and replace the inlet will be considered incidental.  If it is possible to cast in place a new inlet top without removing existing asphalt, but the contractor elects to use a pre-cast inlet top, all asphalt repair/sealing will be considered incidental. Any asphalt repair necessary to re-establish the grade of road at a sunken inlet will be paid separately. Any depth of replacement exceeding 16” will be paid separately with the depth surcharge item. Depth will be measured from bottom of new cast in place concrete, or bottom of grout bed under new pre-cast inlet top, to top of new inlet.

Type M Inlet, Repair (Each) estimated 7
Type M Inlet, Depth Surcharge (Per Inch) 20 inches 
Type M Inlet, Asphalt Surcharge (Per Cu. Ft.) 7

Type S Inlet, Repair (Each) estimated 1
Type S Inlet, Depth Surcharge (Per Inch)  3
Type S Inlet, Asphalt Surcharge (Per Cu. Ft.) 1

Type C Inlet, Repair (Each) estimated 41 
Type C Inlet, Depth Surcharge (Per Inch) 80
Type C Inlet, Asphalt Surcharge (Per Cu. Ft.)  41

Type D-H Inlet, Repair (Each) estimated 2 
Type D-H Inlet, Depth Surcharge (Per Inch) 6
Type D-H Inlet, Asphalt Surcharge (Per Cu. Ft.) 2