PA Boat Title Specs:

- Size: 8.5" X 11"

- Estimated  order- 20,000/yr

- Paper pre-packaged with the following:

- Watermark – Fourdrinier paper with unique watermark embedded.

- Invisible Fluorescent Security Fibers – 2 different colors of that are embedded into the paper, invisible to the naked eye and viewable only with a U-V light.

- Full Chemical Sensitization – To the 5 families of known chemical alteration agents; oxidants, polar solvents, non-polar solvents, acids or alkalis

- Toner Retention Treatment –  This feature facilitates the bonding of laser printed toner characters to the paper surface to deter mechanical alteration through removal of toner data via tape-lift, scraping or other abrasive techniques

- Ink: face and back printed in PMS 296 Blue and Pantone Yellow.  Inks are heat resistant.

- Security Features: Logoline, Iridescent Printing face and back, control number on back (no missing numbers allowed). Document is to include pantograph feature that will display the word VOID if attempt to copy is performed. High Resolution Border is to be included on document as well.

- Starting Inventory Control Number:  To Be Determined…  [NO MISSING NUMBERS]