PA Dept of State				Professional License Certificates with ID Cards

Quantity Requested: 500,000 estimated annual quantity

Description: Laser printed cut sheet printed on security paper

Flat Size: 8 ½ x 11

Paper: 28lb White Security paper.   Paper must contain the following features.

Unique Watermark – Created by the Fourdrinier (dandy-roll) papermaking process, this overall design is pressed into the wet paper, displacing some fibers thereby achieving various levels of light transmission which become visible from either side as a two-dimensional watermark which cannot be photocopied or scanned, removed or corrupted.  Watermark is therefore a unique and major deterrent to counterfeiting.  Watermark design is to be unique to the vendor and not available commercially.

Invisible Fluorescent Security Fibers – This paper should contain 2 different colors of fibers (blue and yellow-green) that are embedded into the paper, invisible to the naked eye and viewable only with a U-V light. This feature therefore cannot be photocopied or scanned and is valuable as an additional tool in determining document authenticity.

Full Chemical Sensitization – Conservator paper pulp contains chemical reagents to the 5 families of known chemical alteration agents. If chemicals from the families of oxidants, polar solvents, non-polar solvents, acids or alkalis are applied to attempt localized chemical alteration, noticeable colored stains will appear through the paper and be visible from either side.

Toner Retention Treatment – If the document is for a laser printed end-use, it is recommended that at least the front of the paper be treated with a security level toner retention feature.  This feature facilitates the bonding of laser printed toner characters to the paper surface to deter mechanical alteration through removal of toner data via tape-lift, scraping or other abrasive techniques. Conservator FF TA4 security paper contains a unique full-face toner retention treatment (TA4) developed specifically for RR Donnelley for high-speed laser printers such as the Xerox 4635 series and Xerox DP180 as well as  other laser-printers.

Inks:   2/1, PMS 301 Blue and PMS 200 Red on Face, Gray on back.

Consecutive Number: Document contains one consecutive number.   It is made up of 9 digits.   The first two digits make up the year of procurement.   There is a space followed by 7 digits.

Perforations: The ID card printed in the upper left corner it be made removable via perforations surrounding the card.  The cards corners are rounded.   There is full width perforation separating the certificate portion form the balance of the form.

Printed Security Features:

Micro Text: (location and content to be determined at design meeting.) Micro text is a line of micro- printed text readable under magnification.  Line will appears solid or jagged when reproduction is attempted.

High Resolution Border:  A design for the border that is artistic and comprised of clear and unbroken lines.  The fine lines in these designs may appear blurred or indistinct when photocopied.

Iridescent Printing:   A Technique that utilizes two print units to take two PMS ink colors and blends them on press.  The Dept of State license paper blends blue into red on the ID card and Blue into Red into Blue on the certificate.

Alpha Lines:  The security feature is located on the reverse side.  It is a security background and the design is comprised of a combination of text lines of varying widths and spacing.  The purpose it to provide a deterrent against attempts to cut and paste critical data from one document to another.

Void Pantograph:  A current up to date VOID pantograph feature must be included in the final design.  This feature will produce the word “COPY” when the document is copied.

Packaging:  Forms must be packed 2000 per carton, 250 per shrink-wrap and 72000 per pallet.  Forms must pack face down with low numbers on top.  Each package to have a label showing the consecutive numbers contained in that package.

Storage and Delivery:  The forms must be stored in a vendor owned warehouse.   The Department will call during the year to arrange delivery of ONE pallet of certificates at a time.  The Department has a standard loading dock.   The delivery vehicle must have a pallet jack.   Inside delivery is required.  The cost for all of these services must be included in the price of the documents.

Bottom of Form