Commonwealth of Pennsylvania

Department of Transportation

# DURABLE PAVEMENT MARKINGS

February 23, 2009

1.	SCOPE

This specification covers the evaluation of the following retroreflective durable pavement marking materials that are applied on the National Transportation Product Evaluation Program (NTPEP) test deck conducted in Pennsylvania:

- Epoxy

- Cold Plastic

- Methyl-Methacrylate (MMA)

- Hot Thermoplastic

- Preformed Thermoplastic

- Polyester

- Polyurea

- Other Types – as recommended by the manufacturer unless specified by the Department

2.	MATERIALS

  - Color.  The pavement markings shall be available in both white and yellow.  Upon product acceptance, the initial unbeaded, finished colors shall satisfy the following chromaticity coordinates:

# Table 1.  Chromaticity Coordinates

| Color | 1 | 2 | 3 | 4 |
| --- | --- | --- | --- | --- |
|  | X1 | Y1 | X2 | Y2 | X3 | Y3 | X4 | Y4 |
| White | 0.330 | 0.370 | 0.355 | 0.345 | 0.310 | 0.300 | 0.285 | 0.325 |
| Yellow | 0.515 | 0.465 | 0.505 | 0.430 | 0.440 | 0.415 | 0.420 | 0.443 |

  - Environmental Issues.  Each manufacturer shall formulate all pavement-marking materials based on their specifications except that the marking materials shall have pigments that during the handling, application and removal of these materials, worker exposure to these products shall not exceed chemical exposure limits as indicated in OSHA 29 CFR 1910. The composition of these products shall be compatible with all conventional application equipment available. The pavement marking materials shall be free from all dirt and foreign objects.

  - Glass Beads.  Apply reflective glass beads Type A, B, C, or D conforming to Department’s Specification Publication 408, Section 1103.14. Rates and material combinations shall be as tested by Department forces on an applicable AASHTO/NTPEP test deck sited in Pennsylvania.

3.	APPLICATION

  - General.  Pavement markings shall be readily applied by the equipment or methods recommended by the manufacturer.

  - Glass Beads.  Except for cold plastic tape markings, the application rate of glass beads by drop-on or pressure methods shall be as recommended by the manufacturer unless specified by the Department by prior AASHTO/NTPEP testing.

  - Application Thickness.  The installed thickness of durable markings shall be as follows:

- Epoxy – 20 mils to 30 Mils

- Cold plastic – 60 mils to 90 Mils

- MMA – 20 mils to 30 Mils

- Hot Thermoplastic – 90 mils to 120 Mils

- Hot Thermoplastic (spray) – 30 mils to 50 Mils

- Preformed Thermoplastic – 90 mils to 125 Mils

- Polyester – 15 mils to 20 Mils

- Polyurea – 20 mils to 30 Mils

- Other types – as recommended by the manufacturer unless specified by the Department

4.	TESTING

  - Number of Test Sites.  For testing purposes, the manufacturer or manufacturer’s representative shall install test lines on both concrete and bituminous roadways as required by NTPEP policies.  Separate test lines shall be installed for each color of each material.  Pavement markings installed on concrete and bituminous surfaces will be evaluated and approved separately for each type and color based on the requirements of the Department's Test Deck specifications.

  - Retroreflectivity Readings.  Retroreflective readings of each line will be taken once a month during the first year after installation and quarterly during the next 2 years.  Retroreflectivity will be measured in millicandelas per square meter per lux (mcd/m2/lux) using a 30-meter Department retroreflectometer.  Readings will be made adjacent to the centerline or lane line (outside the normal travel path of vehicles) and in the wheel path.

  - Durability Ratings.  Durability readings will be evaluated subjectively on a scale of “0” to “10,” where “0” means that the marking does not exist, a “10” means that the marking is completely intact, and intermediate values such as a “5” means that the marking is only 50 percent present.

- APPROVAL

5.1	Types of Approvals.  Materials that satisfy the 2-year minimum retroreflectivity and durability values after 2 years on the test deck will be given a “provisional approval” for sale and use in the Commonwealth (materials may also be given “provisional approval” after the second winter but before the full 2 years if the material satisfies the requirements in the row titled “After 2nd winter” in Table 2), and after 3 years on the test deck will be given full approval for sale and use in the Commonwealth.

- Materials which meet or exceed the retroreflectivity (RR) and durability (D) values as included in Table 2 at the centerline location will be approved for use as centerlines, lane lines and edge lines.

- Materials which meet or exceed the retroreflectivity (RR) and durability (D) values as included in Table 2 at both the centerline and wheel track locations will also be approved for use as crosswalks, stop lines, legends and crosshatching.

# Table 2.  Minimum Retroreflectivity and Durability Values

| Duration | Centerline Location | Wheel Track Location |
| --- | --- | --- |
| Initial | RR = As specified in Pub 408* D = 10 | RR = As specified in Pub 408* D = 10 |
| After 2nd winter** | RR = 165 mcd/m2/lux for white 155 mcd/m2/lux for yellow D = 8 | RR = 120 mcd/m2/lux for white 100 mcd/m2/lux for yellow D = 7 |
| 2 years | RR = 150 mcd/m2/lux for white 135 mcd/m2/lux for yellow D = 8 | RR = 100 mcd/m2/lux for white 90 mcd/m2/lux for yellow D = 7 |
| 3 years | RR = 100 mcd/m2/lux for white 85 mcd/m2/lux for yellow D = 6 | RR = 70 mcd/m2/lux for white 60 mcd/m2/lux for yellow D = 6 |

*  Materials not listed in Pub 408 shall have an initial minimum retroreflectivity of

300 mcd for white and 250 mcd for yellow.

**  These values are only applicable for issuing a provisional approval.

5.2	Changes in Composition.  Manufacturers must notify the Department of any change that has been made to an approved material, physical or chemical, so that the Department can determine if retesting is necessary or if the approval should be revised.

_________________________________

James P. Tenaglia, P.E., Chief

Risk Management and Administrative Services Division

Bureau of Highway Safety and Traffic Engineering